# SPECIFICATION OF BASIC VICTORIA BLUE B DYE

| Product Name | Basic Victoria Blue B Dye |
| --- | --- |
| C. I. Constitution | Basic Blue 26 |
| C.A.S. NO. | (2580 – 56 – 5) |
| Colour Index Number | 44045 |
| Molecular weight | 506.1 |
| Molecular Formula | C33H32N3Cl |
| M.K. Contain | 1.5 |
| Physical Form | Powder |
| Color Appearance | Navy Blue |
| Odor | Odorless |
| Solubility in Water | Insoluble |
| Insoluble | 0.5%max. |
| pH of 1 % Solution | 2.8 |
| Color Strength | 100 % (± 1 %) Against standard |
| Moister Content | 1 % W/W Max. |
| Standard Packing | 25 Kgs. in M.S.Drum / Plastic Carboy |
| Bulk Density (Typical) | Loose : 0.625 Settled : 0.818 |
| Shade on Paper | Reddish Blue Trace difference on either side |
| Application | Dyeing of wool, silk, jute and paper. Pigment for leather & Printing inks etc. |